PYROSLEEVE PGH.20/ROS

Red Oxide Silicone Coated Glass Fibre Sleeving

PYROSLEEVE PGH.20/ROS is manufactured from ‘E’ glass fibre yarn knitted to form a sleeve and coated with high grade iron oxide silicone elastomer rubber.

PGH.20/ROS possesses outstanding characteristics making it ideal for protecting hose assemblies, cables, and wires.

- High flexibility

- Continuous protection at an operating temperature of 250 deg. C

- Ability to  withstand a molten metal splash at 1200 deg. C

- Highly resistant to most oils, hydraulic fluids, fuels, acids and alkalis

- When exposed to flame the high grade rubber will form a protective SiO2 layer

- Health & Safety - Provides personnel with protection against burns from hot hoses, steam lines etc.

- Helps to reduce energy loss by retaining heat within pipework

- Excellent flame resistance

- Excellent abrasion resistance

PYROSLEEVE PGH.20/ROS

Red Oxide Silicone Coated Glass Fibre Sleeving

Available sizes                                      Characteristics

| Nominal inside diameters (mm) |  |  |
| --- | --- | --- |
| 10 | Effect of heat | Will not burn. Retains 75% tensile @ 340°C |
| 12 |  |  |
| 16 |  |  |
| 20 |  |
| 22 | Effects of acids & alkalis | Resistant to acids is fair. Resistance to Alkalis is good |
| 25 |  |  |
| 28 |  |  |
| 32 |  |
| 35 | Silicone rubber Durometer, Shore A Initial Aged 240hrs @ 200°C |  |
| 38 |  |  |
| 41 |  | 875 |
| 44 |  | 800 |
| 50 |  |
| 57 | Dielectric Strength | 30Kv + |
| 63 |  |
| 70 | Tensile Strength | 400,000 – 500,000 psi |
| 76 |  |  |
| 83 | Elastic Recovery | 100% |
| 89 |  |
| 95 | Specific Gravity | 2.54 – 2.69 |
| 102 |  |
| 114 | Effect of bleaches & solvent | unaffected |
| 127 |  |  |

Standard method of Supply : 15M coils